Reviewers:  Use this special for massive concrete units (6’x6’x6’) footings or column diameters >= 6'-0" (1825 mm).

COLD WEATHER CONCRETING IN MASSIVE PIERS AND ABUTMENTS	9/2/04

1.0  Description.  This work shall consist of constructing massive concrete piers and abutments.

2.0  Construction Requirements.

2.1  When curing the sections of the river pier footings and bases directly above the footings, cold weather concreting in Sec 703 shall be modified by the below requirements.  Provisions shall be made in these sections to insert a thermal probe by installation of a galvanized steel conduit or other methods as approved by the engineer.

(a)  When curing is complete on the river pier footings and bases directly above the footings, the temperature of the surrounding air shall be reduced gradually at a rate not exceeding 25°F (14°C) in 24 hours, until 14 days after placement.

(b)  If insulated forms are used for curing, the insulated forms shall not be removed until the temperature differential between the center of the concrete mass and surrounding air does not exceed 20°F (11°C).  The insulated forms will not be required to be left in place beyond 14 days after placement.

3.0  Method of Measurement.  No measurement will be made.

4.0  Basis of Payment.  Payment for the above described work, including all material, equipment, labor and any other incidental work necessary to complete this item, will be considered completely covered by the contract unit price for the concrete.