CLEANING, LUBRICATING AND COATING EXISTING BEARINGS	5/29/12

1.0 Description.  This work shall consist of raising and supporting the existing girders as required to inspect, clean, lubricate and coat existing bearings as specified on the plans and as directed by the engineer.

2.0  Construction Requirements.

2.1  Raising and Supporting the Superstructure.  Before commencing operations, the contractor shall submit to the engineer for review the method and sequence of operation proposed to be used in performing this work.  The contractor shall exercise caution when supporting the structural steel and shall raise the girders the minimum extent necessary to perform this work.  Raising the girders at the bents and piers shall be done simultaneously to prevent any damage to the adjoining steel and concrete deck.  The lifting operation shall be done only when authorized, but such authorization shall not relieve the contractor of responsibility for the safety of the operation or for damage to the structure.  Any damage caused by the contractor’s operations shall be repaired at the contractor’s expense as approved by the engineer.

2.2  Bearing Inspection and Repair.  After the structural members are supported, each bearing shall be inspected for deterioration.  Any or all portions of the deteriorated bearings shall be replaced as determined by the engineer.  When required to remove a bearing, removal of the bearing shall cause no damage to the existing anchor bolts in the concrete beam.  Prior to removal or disassembly, all bearings shall be match marked for reassembly at ends of each piece by stamping an identification number in the metal with a steel stencil.  All existing bearing material determined to be replaced shall be disposed of by the contractor in accordance with Sec 202.

2.3  Cleaning, Lubricating and Coating.  Bearings shall be cleaned in accordance with Sec 1081.  After cleaning and just prior to resetting the bearings, contact surfaces between the bearing pin and cradle shall be given a heavy coat of a graphite grease with a minimum of twenty percent graphite.  After bearings are reset, the bearings shall receive a final cleaning and a prime coat.  The final coat shall be applied when the existing structural steel is coated.  Coating of bearings shall be as indicated for coating existing steel as specified in the contract documents.

3.0  Method of Measurement.  Measurement for cleaning, lubricating and coating existing bearings will be made per each.

4.0  Basis of Payment.  When required, payment for furnishing any new bearing material will be in accordance with Sec 109.  Payment for the above described work, including all material, equipment, labor and any other incidental work necessary to complete this item, will be considered completely covered by the contract unit price for “Cleaning, Lubricating and Coating Bearing”.