Reviewers:  To be used only with permission from Review Section.

COATING GALVANIZED SLAB DRAINS		10/25/05

1.0  Description.  The portions of the slab drains and drain supports extending below the slab shall be shop or field coated before erection in accordance with the following provision to match the color of the coating finish applied to the exterior face of the girders.

2.0  Materials.  All material shall be in accordance with Division 1000, Material Details, and specifically as follows.

| Item |  | Section |
| --- | --- | --- |
| Structural Steel Fabrication |  | 1080 |
| Coating of Structural Steel |  | 1081 |

3.0  Fabrication.

3.1  Slab drains and drain supports shall be as shown on the bridge plans.  Slab drains and drain supports shall be hot-dip galvanized after fabrication.  Precautions shall be taken with the galvanizing to ensure that the slab drains are not water or chromate quenched after galvanizing.

3.2  Coating shall not proceed until at least 48 hours after galvanizing.  Galvanized surfaces to be coated shall be cleaned to SSPC-SP-1 and followed by a light abrasive brush blast to meet SSPC-SP-7.  Slab drains shall be coated in accordance with the requirements of Sec 1081 for the system as noted on the plans which includes the intermediate and finish coats.  When System H is required, the surfaces to be coated shall be treated with a tie coat after brush blasting.  The tie coat shall be in accordance with the recommendations from the manufacturer of the intermediate and finish coat system.

3.3  During the coating of the slab drains, all surfaces of concrete and other areas not to receive the coating shall be protected from drippings of coating material and over spray.  All coating material on surfaces not to be coated shall be immediately cleaned to remove all coating material to the satisfaction of the engineer.

4.0  Method of Measurement.  Measurement for slab drains will be made per each.

5.0  Basis of Payment.  Payment for the above described work, including all material, equipment, labor and any other incidental work necessary to complete this item, will be considered completely covered by the contract unit price for “Slab Drain”.