CONSTRUCTION OBSERVATION PROGRAM (COP)

REQUIRED TESTS

AND

CERTIFICATIONS

Excavation and Embankment, MO-152

Name	Number	Frequency	Tolerances/Acceptance

Standard Proctor	ASTM D-698	Minimum one 	N/A

per soil type

Field Soil Density	ASTM D-2922	[See Note 2]	MO-152, 152-2.2 & 152-2.5

Moisture Content by	ASTM D-3017	[See Note 2]	MO-152, 152-2.2 & 152-2.5.

Nuclear Method				Shall be within  2% of the

optimum moisture content.

Soil Smoothness	MO-152, 152-2.9	As required to assure	See note 1

compliance with

specifications.

Note 1: Areas upon which aggregate base course will be placed:

smoothness and grade - no deviation in excess of 1/2" when tested with a 16' straightedge applied parallel and at right angles to centerline, or shall not be more than 0.05 foot from true grade as established by grade hubs or pins.

Runway safety areas, intermediate and other designated areas:

smoothness and grade - the surface shall not vary more than 0.10 foot from true grade as established by grade hubs or pins.

* * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * *

Note 2:  Insert the frequency from MO-152, Paragraph 152-2.5.

* * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * *

## Fly Ash Treated Subgrade, MO-155

Name	Number	Frequency	Tolerances/Acceptance

Standard Proctor	ASTM D-698	Minimum one	N/A

per soil type

Fly Ash	MO-155, 155-3.2	As required to assure	Shall not be below nor more

compliance with	0.5% above the specified rate.

specifications.

Field Soil Density	ASTM D-2922	Minimum one for	MO-155, 155-5.7

each 750 S.Y.	Minimum density, 95%.

Moisture Content by	ASTM D-3017	Minimum one for	MO-155, 155-5.6

Nuclear Method		each 750 S.Y.	Shall not be below nor more

than 2% above the optimum

moisture content.

Soil Smoothness	MO-155, 155-5.8	As required to assure 	Shall not vary more than 3/8”

compliance with	when tested with a 16’

specifications.	straightedge.

Soil Thickness	MO-155, 155-5.9	Minimum one for	Not deficient more than 1/2”.

each 300 S.Y.

Curing	MO-155, 155-5.8	N/A	Maintain in a thorough and

continuously moist condition

by sprinkling or apply a 2”

layer of earth on the completed

course and maintain in a moist

condition.

Required Material Certifications

Fly Ash (Class C)	ASTM C-618	As needed	MO-155, 155-2.1

Water	AASHTO T26	As needed	Clean, clear, free of sewage,

vegetable matter, oil, acid and

alkali. Water known to be

potable does not require any

testing.

Crushed Aggregate Base Course, MO-209

Aggregate.   All materials for aggregate base shall conform to the requirements of the 2004 (MSSHC), Section 304, for Type 5 Aggregate.

Material Acceptance.   The ledge stone from which the aggregate base will be produced has to have source approval from the Missouri Department of Transportation (MoDOT). Prior to use of materials, the contractor shall submit the current MoDOT source approval letter to the Engineer for the materials proposed for use during construction. Source approval granted for “all types of highway construction” (Product Code 1005CACP) constitutes approval for all uses. Source approval granted for “all types except PCCP” (Product Code 1005CACM) comprises approval for all uses except portland cement concrete pavement. Source approval obtained for “all types except PCCP & PCCM” (Product Code 1002CAAC) is considered to be approval for all uses except portland cement concrete.

The contractor shall submit certified test reports to the Engineer for the gradation of the aggregate base. The certification shall show the appropriate AASHTO test for the material, the test results, and a statement that the material passed or failed. The aggregate shall be sampled and tested for gradation using the following procedures:

1.	Sampling Aggregates. Sampling shall be in accordance with AASHTO T 2.

2.	Sieve Analysis of Fine and Coarse Aggregate. The aggregate shall be tested in accordance with AASHTO T 27 and shall meet the gradation requirements of the MSSHC, Section 1007.3.

3.	Material Passing No. 200 Sieve. The aggregate shall be tested in accordance with AASHTO T 11 and meet the requirements of the MSSHC, Section 1007.3.

In lieu of the above gradation testing requirements, the contractor may provide documentation from MoDOT (District Materials Office) indicating that the material meets specification requirements.

The Engineer may request samples for testing, prior to and during production, to verify the quality of the materials and to ensure conformance with the applicable specifications.

Other Testing Requirements

Name	Number	Frequency	Tolerances/Acceptance

Standard Proctor	ASTM D 698	1	N/A

Field Density	ASTM D 1556	2 per lot	100% of D 698 is required.

ASTM D 2167		Calibrate gauge in

ASTM D 2922		accordance with Annex

MO-209, 209-3.5		A1 of referenced ASTM.

Moisture Content by	ASTM D 3017	2 per lot	Shall not be below nor more

Nuclear Method	MO-209, 209-3.4		than 1-1/2 % above the

MO-209, 209-3.5		optimum moisture content

during placing operations.

Random Sampling	ASTM D 3665		N/A

MO-209, 209-3.5	2 per lot (density)

MO-209, 209-3.8	4 per lot (thickness)

Name	Number	Frequency	Tolerances/Acceptance

Smoothness	MO-209, 209-3.7	As needed	3/8" per 16' straightedge

Thickness	MO-209, 209-3.8	4 per lot	Shall be within  1/2" of the

design thickness.

Plant Mix Bituminous Pavement, MO-401F

Aggregates.   Coarse and fine aggregates for plant mix bituminous pavement shall conform to the requirements of the 2004 (MSSHC), Section 401.

Aggregate Material Acceptance.   The ledge stone from which the coarse aggregate will be produced has to have source approval from the Missouri Department of Transportation (MoDOT). Prior to use of materials, the contractor shall submit the current MoDOT source approval letter to the Engineer for the materials proposed for use during construction. Source approval granted for “all types of highway construction” (Product Code 1005CACP) constitutes approval for all uses. Source approval granted for “all types except PCCP” (Product Code 1005CACM) comprises approval for all uses except portland cement concrete pavement. Source approval obtained for “all types except PCCP & PCCM” (Product Code 1002CAAC) is considered to be approval for all uses except portland cement concrete.

For fine aggregate, the contractor shall submit to the Engineer a certification from the supplier that the fine aggregate complies with the specification requirements. The certification statement shall be signed by an authorized representative of the supplier and shall be substantially as follows:

“This certifies that the fine aggregate being supplied for this project complies with Section 1005.3 of the 2004 Missouri Standard Specification for Highway Construction.”

The Engineer may request samples for testing, prior to and during production, to verify the quality of the materials and to ensure conformance with the applicable specifications.

Bituminous Material Acceptance.   Bituminous material shall conform to the requirements of the 2004 MSSHC, Section 401. The grade of the asphalt cement shall be PG 64-22.

The supplier shall guarantee by certification that bituminous material complies with the specification requirements. The supplier shall furnish the truck driver a copy of the bill of lading, manifest or truck ticket that is available to the engineer at destination prior to unloading. The engineer at the source is also to be furnished a copy. The bill of lading, manifest or truck ticket shall show the following information regarding the shipment: type and grade of material, specific gravity at 60 F (15.6 C), net gallons (liters), consignee, truck number, identification number, weight (mass) of truck before and after loading, destination, date loaded, name and location of the source, and a certification statement. The certification statement shall be signed by an authorized representative of the supplier and shall be substantially as follows:

“This certifies that the bituminous material in this shipment complies with MoDOT specifications for the grade specified and the weights (masses) shown hereon were obtained on MoDOT approved scales and are correct within the specified scale requirements.”

Prior to use of bituminous materials, the contractor shall provide the engineer the above certified bill of lading, manifest or truck ticket for each load to be incorporated into the project.

Other Testing Requirements

Testing Laboratory - The laboratory used to develop the job mix formula shall meet the requirements of ASTM D 3666.  A certification signed by the manager of the laboratory stating that it meets these requirements shall be submitted to the Engineer prior to the start of construction.

Mix Design - The proposed mixture shall be compacted and tested by the contractors approved laboratory in accordance with AASHTO T 245. The number of blows with the compaction hammer shall be 35. The submitted mix design by the contractor shall meet the requirements of MO-401F, 401-3.1.  In addition, production shall not begin until the job mix formula is approved in writing by the Engineer.

Name	Number	Frequency	Tolerances/Acceptance

Sieve Analysis of 	AASHTO T 27	At Engineers	MO Standard Specification

Fine and Coarse			Discretion	for Highway Construction,

Aggregate					Section 401.3 for BP-1

(Total aggregate for mixture).

Random Sampling	ASTM D 3665 	As needed	N/A

Mat Density	ASTM D 2726	4 per lot	MO-401F, 401-5.2B1

or D 1188

Joint Density	ASTM D 2726	4 per lot	MO-401F, 401-5.2B2

or D 1188

Thickness of Cores	MO-401F 	4 per lot	401-5.2B3

Smoothness	MO-401F	401-5.2B4	401-5.2B4, 401-8.1B

Grade	MO-401F	401-5.2B5	401-5.2B5

Contractor Quality Control Program  (The following items should be monitored by the engineer to ensure compliance with the specification).

Quantitative Extraction 	ASTM D 2172

of Bitumen

Mechanical Analysis of	AASHTO T 30

Extracted Aggregate

Sieve or Screen Analysis 	ASTM C 136

of Fine and Coarse

Aggregates

Total Moisture Content	ASTM C 566

of Aggregate by Drying

Moisture or Volatile 	ASTM D 1461

Distillates in Bituminous

Paving Mixtures

Temperatures:	Temperatures shall be checked at least four times per lot, at necessary locations to determine the temperatures of the dryer, the bitumen in the storage tank, the mixture at the plant, and the mixture at the job site.

In-Place Density Monitoring:	The contractor shall conduct any necessary testing to ensure that the specified density is being achieved.

Plant Mix Bituminous Pavement, MO-401S

Aggregates.   Coarse and fine aggregates for plant mix bituminous pavement shall conform to the requirements of the 2004 (MSSHC), Section 401.

Aggregate Material Acceptance.   The ledge stone from which the coarse aggregate will be produced has to have source approval from the Missouri Department of Transportation (MoDOT). Prior to use of materials, the contractor shall submit the current MoDOT source approval letter to the Engineer for the materials proposed for use during construction. Source approval granted for “all types of highway construction” (Product Code 1005CACP) constitutes approval for all uses. Source approval granted for “all types except PCCP” (Product Code 1005CACM) comprises approval for all uses except portland cement concrete pavement. Source approval obtained for “all types except PCCP & PCCM” (Product Code 1002CAAC) is considered to be approval for all uses except Portland cement concrete.

For fine aggregate, the contractor shall submit to the Engineer a certification from the supplier that the fine aggregate complies with the specification requirements. The certification statement shall be signed by an authorized representative of the supplier and shall be substantially as follows:

“This certifies that the fine aggregate being supplied for this project complies with Section 1005.3 of the 2004 Missouri Standard Specification for Highway Construction.”

The Engineer may request samples for testing, prior to and during production, to verify the quality of the materials and to ensure conformance with the applicable specifications.

Bituminous Material Acceptance.   Bituminous material shall conform to the requirements of the 2004 MSSHC, Section 401. The grade of the asphalt cement shall be PG 64-22.

The supplier shall guarantee by certification that bituminous material complies with the specification requirements. The supplier shall furnish the truck driver a copy of the bill of lading, manifest or truck ticket that is available to the engineer at destination prior to unloading. The engineer at the source is also to be furnished a copy. The bill of lading, manifest or truck ticket shall show the following information regarding the shipment: type and grade of material, specific gravity at 60 F (15.6 C), net gallons (liters), consignee, truck number, identification number, weight (mass) of truck before and after loading, destination, date loaded, name and location of the source, and a certification statement. The certification statement shall be signed by an authorized representative of the supplier and shall be substantially as follows:

“This certifies that the bituminous material in this shipment complies with MoDOT specifications for the grade specified and the weights (masses) shown hereon were obtained on MoDOT approved scales and are correct within the specified scale requirements.”

Prior to use of bituminous materials, the contractor shall provide the engineer the above-certified bill of lading, manifest or truck ticket for each load to be incorporated into the project.

Other Testing Requirements

Testing Laboratory - The laboratory used to develop the job mix formula shall meet the requirements of ASTM D 3666.  A certification signed by the manager of the laboratory stating that it meets these requirements shall be submitted to the Engineer prior to the start of construction.

Mix Design - The proposed mixture shall be compacted and tested by the contractors approved laboratory in accordance with AASHTO T 245. The number of blows with the compaction hammer shall be 35. The submitted mix design by the contractor shall meet the requirements of MO-401S, 401-3.1.  In addition, production shall not begin until the job mix formula is approved in writing by the Engineer.

Name	Number	Frequency	Tolerances/Acceptance

Sieve Analysis of 	AASHTO T 27	At Engineers	MO Standard Specification

Fine and Coarse		Discretion	for Highway Construction,

Aggregate			Section 401.3 for BP-1

(Total aggregate for mixture).

Random Sampling	ASTM D 3665 	As needed	N/A

Mat Density	ASTM D 2726	4 per lot	MO-401S, 401-5.2B1

or D 1188

Joint Density	ASTM D 2726	4 per lot	MO-401S, 401-5.2B2

or D 1188

Thickness of Cores	MO-401S	4 per lot	401-5.2B3

Smoothness	MO-401S	401-5.2B4	401-5.2B4, 401-8.1B

Grade	MO-401S	401-5.2B5	401-5.2B5

Contractor Quality Control Program  (The following items should be monitored by the engineer to ensure compliance with the specification).

Quantitative Extraction 	ASTM D 2172

of Bitumen

Mechanical Analysis of	AASHTO T 30

Extracted Aggregate

Sieve or Screen Analysis 	ASTM C 136

of Fine and Coarse

Aggregates

Total Moisture Content	ASTM C 566

of Aggregate by Drying

Moisture or Volatile 	ASTM D 1461

Distillates in Bituminous

Paving Mixtures

Temperatures:	Temperatures shall be checked at least four times per lot, at necessary locations to determine the temperatures of the dryer, the bitumen in the storage tank, the mixture at the plant, and the mixture at the job site.

In-Place Density Monitoring:	The contractor shall conduct any necessary testing to ensure that the specified density is being achieved.

Portland Cement Concrete Pavement, MO-501

Aggregates.   Coarse and fine aggregates for Portland cement concrete shall conform to the requirements of the 2004 (MSSHC), Section 501, for Pavement class concrete.

Material Acceptance.   The ledge stone from which the coarse aggregate will be produced has to have source approval from the Missouri Department of Transportation (MoDOT). Prior to use of materials, the contractor shall submit the current MoDOT source approval letter to the Engineer for the materials proposed for use during construction. Source approval granted for “all types of highway construction” (Product Code 1005CACP) constitutes approval for all uses. Source approval granted for “all types except PCCP” (Product Code 1005CACM) comprises approval for all uses except portland cement concrete pavement. Source approval obtained for “all types except PCCP & PCCM” (Product Code 1002CAAC) is considered to be approval for all uses except portland cement concrete.

The contractor shall submit certified test reports to the Engineer for the gradation of the coarse aggregate. The certification shall show the appropriate AASHTO test for the material, the test results, and a statement that the material passed or failed. The aggregate shall be sampled and tested for gradation using the following procedures:

1.	Sampling Aggregates.  Sampling shall be in accordance with AASHTO T 2.

2.	Sieve Analysis of Fine and Coarse Aggregate.  The coarse aggregate shall be tested in accordance with AASHTO T 27 and meet the applicable gradation requirements of the MSSHC, Section 1005.2.

3.	Material Passing No. 200 Sieve.  The portion of material passing the No. 200 sieve shall be tested in accordance with AASHTO T 11 and meet the requirements of the MSSHC, Section 1005.2.

In lieu of the above gradation testing requirements, the contractor may provide documentation from MoDOT (District Materials Office) indicating that the material meets specification requirements.

For fine aggregate, the contractor shall submit to the Engineer a certification from the supplier that the fine aggregate complies with the specification requirements. The certification statement shall be signed by an authorized representative of the supplier and shall be substantially as follows:

“This certifies that the fine aggregate being supplied for this project complies with Section 1005.3 of the 2004 Missouri Standard Specification for Highway Construction.”

The Engineer may request samples for testing, prior to and during production, to verify the quality of the materials and to ensure conformance with the applicable specifications.

Other testing requirements

Testing Laboratory - The laboratory used to develop the job mix formula shall meet the requirements of ASTM C 1077. A certification signed by the manager of the laboratory that it meets these requirements shall be submitted to the engineer prior to the start of the mix design.

Mix Design - The proposed mixture shall be designed by the contractor's approved laboratory by absolute volume methods or an optimized mix design. The submitted mix design by the contractor shall meet the requirements of MO-501, 501-3.1. In addition, production shall not begin until the mix design is approved in writing by the Engineer.

Name	Number	Frequency	Tolerances/Acceptance

Ready Mixed Concrete 	ASTM C 94	As required	N/A

Random Sampling	ASTM D 3665	As needed	N/A

Sampling Concrete	ASTM C 172	1 per sublot	N/A

(AASHTO T 141)

Making and Curing 	ASTM C 31	8 per lot	N/A

Concrete Specimens		2 per sublot

Slump	ASTM C 143	1 per sublot	MO-501, 501-6.2, 6.3, 6.4

(AASHTO T 119)

Air Content	ASTM C 231	1 per sublot	MO-501, 501-6.2, 6.3, 6.4

(AASHTO T 152)

Temperature	ASTM C 1064	1 per sublot	MO-501, 501-4.7

Compressive Strength	ASTM C 39 	8 per lot	MO-501, 501-5.1, 5.2

2 per sublot

Outliers 	ASTM E 178	8 per lot	MO-501, 501-5.1D

Thickness of Cores	ASTM C 174	4 per lot	MO-501, 501-5.2

Smoothness	MO-501	501-5.2E(3)	501-5.2E(3)

Grade		MO-501 	501-5.2E(4)	501-5.2E(4)

Edge Slump	MO-501 	501-5.2E(5)	501-5.2E(5)

Dowel Bar Alignment	MO-501 	501-5.2E(6)	501-5.2E(6)

Required Material Certifications

Cement		AASHTO M 85	As needed	MSSHC Section 1019

Fly Ash		AASHTO M 295	As needed	MSSHC Section 1018

Slag		AASHTO M 302	As needed	MSSHC Section 1017

Concrete Joint Sealer	AASHTO M 173	As needed	MSSHC Section 1057

Premolded Joint Filler	AASHTO M 213	As needed	MSSHC Section 1057

Steel Wire Fabric	AASHTO M 55 	As needed	MSSHC Section 1036

or M 221

Dowel and Tie Bars	AASHTO M 31,	As needed	MSSHC Section 1057

M 42 or M 53

Dowel and Tie Bar	MSSHC	As needed	MSSHC Section 1036.3.4

Coating

Name		Number	Frequency	Tolerances/Acceptance

Curing Compound	AASHTO M 148	As needed	MSSHC Section 1055

Air Entrainment	AASHTO M 154	As needed	MSSHC Section 1054

Water Reducer	AASHTO M 194	As needed	MSSHC Section 1054

Type A Only

Retarder	AASHTO M 194	As needed	MSSHC Section 1054

Type B or D

Epoxy Resin	ASTM C 881	As needed	MO-501, 501-2.1

Water	MSSHC	As needed	MSSHC Section 1070

Contractor Quality Control Program (The following items should be monitored by the engineer to ensure compliance with the specification).

Fine Aggregate

Sieve or Screen Analysis of	AASHTO T 27 (ASTM C 136)

Fine and Coarse Aggregates

Total Moisture Content of	AASHTO T 255 (ASTM C 566)

Aggregates by Drying

Coarse Aggregate

Sieve or Screen Analysis of	AASHTO T 27 (ASTM C 136)

Fine and Coarse Aggregates

Total Moisture Content of	AASHTO T 255 (ASTM C 566)

Aggregates by Drying

Test for Slump of Portland 	AASHTO T 119 (ASTM C 143)

Cement Concrete

Test for Air Content	AASHTO T 152 (ASTM C 231)

Sampling Freshly Mixed Concrete	AASHTO T 141 (ASTM C 172)

Structural Portland Cement Concrete, MO-610

Aggregates.   Coarse and fine aggregates for Portland cement concrete shall conform to requirements of the 2004 (MSSHC), Section 501, for Class B concrete.

Material Acceptance.   The ledge stone from which the coarse aggregate will be produced has to have source approval from the Missouri Department of Transportation (MoDOT). Prior to use of materials, the contractor shall submit the current MoDOT source approval letter to the Engineer for the materials proposed for use during construction. Source approval granted for “all types of highway construction” (Product Code 1005CACP) constitutes approval for all uses. Source approval granted for “all types except PCCP” (Product Code 1005CACM) comprises approval for all uses except portland cement concrete pavement. Source approval obtained for “all types except PCCP & PCCM” (Product Code 1002CAAC) is considered to be approval for all uses except portland cement concrete.

The contractor shall submit certified test reports to the Engineer for the gradation of the coarse aggregate. The certification shall show the appropriate AASHTO test for the material, the test results, and a statement that the material passed or failed. The aggregate shall be sampled and tested for gradation using the following procedures:

1.	Sampling Aggregates.  Sampling shall be in accordance with AASHTO T 2.

2.	Sieve Analysis of Fine and Coarse Aggregate.  The coarse aggregate shall be tested in accordance with AASHTO T 27 and meet the applicable gradation requirements of the MSSHC, Section 1005.2.

3.	Material Passing No. 200 Sieve.  The portion of material passing the No. 200 sieve shall be tested in accordance with AASHTO T 11 and meet the requirements of the MSSHC, Section 1005.2.

In lieu of the above gradation testing requirements, the contractor may provide documentation from MoDOT (District Materials Office) indicating that the material meets specification requirements.

For fine aggregate, the contractor shall submit to the Engineer a certification from the supplier that the fine aggregate complies with the specification requirements. The certification statement shall be signed by an authorized representative of the supplier and shall be substantially as follows:

“This certifies that the fine aggregate being supplied for this project complies with Section 1005.3 of the 2004 Missouri Standard Specification for Highway Construction.”

Prior to the use of all other materials (cement, admixtures, reinforcing steel, etc.) proposed for use during construction, the contractor shall submit to the Engineer the appropriate manufacturer’s certification per the 2004 MSSHC indicating that the material meets specification requirements.

The Engineer may request samples for testing, prior to and during production, to verify the quality of the materials and to ensure conformance with the applicable specifications.

Other testing requirements

Name	Number	Frequency	Tolerances/Acceptance

Sampling Concrete	ASTM C 172	One per pour or as 	N/A

required to assure

compliance w/specs.

Name	Number	Frequency	Tolerances/Acceptance

Making and Curing 	ASTM C 31	One set per pour or 	N/A

Concrete Specimens		as required to assure

compliance w/specs.

Slump	ASTM C 143	One per pour or as	4"  maximum

required to assure

compliance w/specs.

Air Content	ASTM C 231	One per pour or as	Minimum 5.0%

required to assure

compliance w/specs.

Temperature	ASTM C 1064	One per pour or as 	MO-610, 610-3.18

required to assure

compliance w/specs.

Compressive	ASTM C 39	One set per pour or	Minimum 3,000 psi

Strength Test		as required to assure	in 28 days.

compliance w/specs

Required Material Certifications

Cement		AASHTO M 85	As needed	MSSHC Section 1019

Fly Ash		AASHTO M 295	As needed	MSSHC Section 1018

Slag		AASHTO M 302	As needed	MSSHC Section 1017

Premolded Joint Filler	AASHTO M 213	As needed	MSSHC Section 1057.1

Reinforcing Steel	AASHTO M 31,	As needed	MSSHC Section 1036.1

42 or 53

Steel Wire Fabric	AASHTO M 55	As needed	MSSHC Section 1036.1

or M 221

Curing Compound	AASHTO M 148	As needed	MSSHC Section 1055

Air Entrainment	AASHTO M 154	As needed	MSSHC Section 1054

Water Reducer	AASHTO M 194	As needed	MSSHC Section 1054

Type A Only

Retarder	AASHTO M 194	As needed	MSSHC Section 1054

Type B or D

Water	MSSHC	As needed	MSSHC Section 1070

# Wire Fence with Steel Posts, MO-161

Required Certification.  The contractor shall furnish manufacturer’s certified test reports including a statement that the materials meet the specification requirements.

# Chain Link Fences, MO-162

Required Certification.  The contractor shall furnish manufacturer’s certified test reports including a statement that the materials meet the specification requirements.

Joint and Crack Resealing-Concrete Pavement, MO-500

Required Certification.  The contractor shall furnish manufacturer’s certified test reports including a statement that the materials meet the specification requirements.

Bituminous Prime Coat, MO-602

Required Certification.  The contractor shall furnish vendor’s certified test reports including a statement that the materials meet the specification requirements.

Bituminous Tack Coat, MO-603

Required Certification.  The contractor shall furnish vendor’s certified test reports including a statement that the materials meet the specification requirements.

# Runway and Taxiway Painting, MO-620

Required Certification.  The contractor shall furnish manufacturer’s certified test reports including a statement that the materials meet the specification requirements.

# Crack and Joint Sealing-Bituminous Pavement, MO-622

Required Certification.  The contractor shall furnish manufacturer’s certified test reports including a statement that the materials meet the specification requirements.

## Pavement Friction Sealcoat Surface Treatment, MO-623

Required Certification.  The contractor shall furnish manufacturer’s certified test reports including a statement that the materials meet the specification requirements.

Pipe for Storm Drains and Culverts, MO-701

Required Certification.  The contractor shall furnish manufacturer’s certified test reports including a statement that the materials meet the specification requirements.

# Pipe Underdrains for Airports, D-705

Required Certification.  The contractor shall furnish manufacturer’s certified test reports including a statement that the materials meet the specification requirements.

# Prefabricated Underdrains, MO-706

Required Certification.  The contractor shall furnish manufacturer’s certified test reports including a statement that the materials meet the specification requirements.

# Manholes, Catch Basins, Inlets, and Inspection Holes, D-751

Required Certification.  The contractor shall furnish manufacturer’s certified test reports including a statement that the materials meet the specification requirements.

# Seeding, MO-901

Required Certification.  The seed shall be grown and processed in the United States or Canada and comply with the requirements of the Missouri Seed Law.

Seed shall be furnished separately or in mixtures in standard containers with the seed name, lot number, net weight, percentages of purity and of germination and hard seed, and percentage of maximum weed seed content clearly marked for each kind of seed. The contractor shall furnish the engineer duplicate signed copies of a statement by the vendor certifying that each lot of seed has been tested by a recognized laboratory for seed testing within 6 months of date of delivery. This statement shall include: name and address of laboratory, date of test, lot number for each kind of seed, and the results of tests as to name, percentages of purity and of germination, and percentage of weed content for each kind of seed furnished, and, in case of a mixture, the proportions for each kind of seed.

Lime.  The quantity of material required to provide the specified pounds of effective neutralizing material per acre shall be determined from the producer or distributor’s certification of analysis furnished by the Director of the Missouri Agricultural Experiment Station, Columbia, Missouri in accordance with the Missouri Agricultural Liming Materials Act. The contractor shall furnish a copy of this certification including a statement that the materials meet the specification requirements.

Agricultural lime furnished as a commercially bagged product, pelletized or otherwise, with a guaranteed product analysis shown on the bag listing the elemental properties and gradation may be accepted on the basis of bag label analysis.

Fertilizer.  The contractor shall furnish a supplier’s certification including a statement that the materials meet the specification requirements or may be accepted on the basis of bag label analysis. Materials shall comply with all applicable Missouri fertilizer laws.

# Mulching, MO-908

Required Certification.  The contractor shall provide the sources and quantities of mulch materials available and furnish representative samples of the materials to be used. These samples may be used as standards with the approval of the Engineer and any materials brought on site, which do not meet these standards, shall be rejected.

# Installation of Airport Rotating Beacon, MO-101

Installation of Airport Beacon Towers, MO-103

Installation of Airport 8 or 12-Foot Wind Cone, MO-107

Installation of Underground Cable for Airports, MO-108

Installation of Airport Transformer Vault and Vault Equipment, MO-109

Installation of Underground Electrical Duct, MO-110

Installation of Precision Approach Path Indicator (PAPI) System, MO-120

Installation of Airport Lighting Systems, MO-125

Required Certification.  The contractor shall furnish airport lighting equipment that conforms to the requirements of cited materials specifications. In addition, where an FAA specification for airport lighting equipment is cited in the plans or specifications, the contractor shall furnish such equipment that is:

a.  Listed in FAA Advisory Circular (AC) 150/5345-53, Airport Lighting Equipment Certification Program, that is in effect on the date of advertisement.

b. Produced by the manufacturer qualified (by FAA) to produce such specified and listed equipment.

All other equipment and materials not covered by the referenced AC shall be subject to acceptance by manufacturer’s certificates of compliance stating that such materials meet the specification requirements, when requested by the Engineer.

Required Testing (General).  The contractor shall perform the following tests in the presence of the Engineer for all electrical systems:

- That all lighting power and control circuits are continuous and free from short circuits.

- That all circuits are free from unspecified grounds.

- That the insulation resistance to ground of all nongrounded series circuits is not less than 50 megohms.

- That the insulation resistance to ground of all nongrounded conductors of multiple circuits is not less than 50 megohms.

- That all circuits are properly connected in accordance with applicable wiring diagrams.

- That all circuits are operable. Tests shall be conducted that include operating each control not less than 10 times and the continuous operation of each lighting and power circuit for not less than 1/2 hour.