ITEM MO-603  BITUMINOUS TACK COAT

DESCRIPTION

603-1.1   This item shall consist of preparing and treating an existing bituminous or concrete surface with bituminous material in accordance with these specifications and in reasonably close conformity with the lines shown on the plans. The bituminous material shall conform to the requirements of the 2004 Missouri Standard Specification for Highway Construction (MSSHC), Section 407--Tack Coat. All construction methods, testing, and acceptance criteria shall be in accordance with the standards included within this Item MO-603.

MATERIALS

603-2.1  BITUMINOUS MATERIALS.   Bituminous material shall conform to the requirements of the 2004 MSSHC, Section 407. The type and grade shall be SS-1, SS-1H, CSS-1, or CSS-1H.

The supplier shall guarantee by certification that bituminous material complies with the specification requirements. The supplier shall furnish the truck driver a copy of the bill of lading, manifest or truck ticket that is available to the engineer at destination prior to unloading. The engineer at the source is also to be furnished a copy. The bill of lading, manifest or truck ticket shall show the following information regarding the shipment: type and grade of material, specific gravity at 60 F, net gallons, consignee, truck number, identification number, weight of truck before and after loading, destination, date loaded, name and location of the source, and a certification statement. The certification statement shall be signed by an authorized representative of the supplier and shall be substantially as follows:

“This certifies that the bituminous material in this shipment complies with MoDOT 	specifications for the grade specified and the weights shown hereon were obtained on 	MoDOT approved scales and are correct within the specified scale requirements.”

Prior to use of bituminous materials, the contractor shall provide the engineer the above certified bill of lading, manifest or truck ticket for each load to be incorporated into the project. If the contractor applies the material prior to receipt of the test reports, payment for the material shall be withheld until they are received. If the material does not pass the specification it shall be replaced at the contractor’s expense.

CONSTRUCTION METHODS

603-3.1  WEATHER LIMITATIONS.   The tack coat shall be applied only when the existing surface is dry and the atmospheric temperature is above 60 F. The temperature requirements may be waived, but only when so directed by the Engineer.

603-3.2 EQUIPMENT.  The Contractor shall provide equipment for heating and applying the bituminous material.

The distributor shall be designed, equipped, maintained, and operated so that bituminous material at even heat may be applied uniformly o variable widths of surface at the specified rate. The allowable variation from the specified rate shall not exceed 10 percent. Distributor equipment shall include a tachometer, pressure gages, volume-measuring devices or a calibrated tank, and a thermometer for measuring temperatures of tank contents. The distributor shall be self-powered and shall be equipped with a power unit for the pump and full circulation spray bars adjustable laterally and vertically.

If the distributor is not equipped with an operable quick shut off valve, the tack operations shall be started and stopped on building paper. The contractor shall remove blotting sand prior to the plant mix bituminous laydown operations at no additional expense to the owner.

A power broom and/or blower shall be provided for any required cleaning of the surface to be treated.

603-3.3  APPLICATION OF BITUMINOUS MATERIAL.   Immediately before applying the tack coat, the full width of surface to be treated shall be swept with a powerbroom and/or airblast to remove all loose dirt and other objectionable material.

Emulsified asphalt shall be diluted by the addition of water when directed by the Engineer and shall be applied a sufficient time in advance of the paver to ensure that all water has evaporated before any of the overlying mixture is placed on the tacked surface.

The asphalt emulsion shall be heated at the time of application to a temperature specified by the Engineer in accordance with the limits provided in Section 1015 of the MSSHC.

The bituminous material including vehicle or solvent shall be uniformly applied with a bituminous distributor at the rate of 0.05 to 0.15 gallons per square yard depending on the condition of the existing surface. The type of bituminous material and application rate shall be approved by the Engineer prior to application.

Following the application, the surface shall be allowed to cure without being disturbed for such period of time as may be necessary to permit drying out and setting of the tack coat. This period shall be determined by the Engineer. The surface shall then be maintained by the Contractor until the next course has been placed. Suitable precautions shall be taken by the Contractor to protect the surface against damage during this interval.

METHOD OF MEASUREMENT

603-4.1  The bituminous material for tack coat shall be measured by the gallon. Volume shall be corrected to the volume at 60 F in accordance with ASTM D 1250 for cutback asphalt, ASTM D 633 for tar, and Table IV-3 of The Asphalt Institute's Manual MS-6 for emulsified asphalt. Water added to emulsified asphalt will not be measured for payment.

BASIS OF PAYMENT

603.5-1   Payment shall be made at the contract unit price per gallon of bituminous tack coat. This price shall be full compensation for furnishing all materials, for all preparation, delivery, and application of these materials, and for all labor, equipment, tools, and incidentals necessary to complete the item.

Payment will be made under:

Item MO-603-5.1      Bituminous Tack Coat--per gallon.