Design a concrete mix

And test how strong it is…

Concrete is used for everything from roadways to buildings, and even countertops.  Equations help, but concrete mix design is usually a trial-and-error process.  In this activity you will be designing a concrete mix using the process in ACI (American Concrete Institute) 211.1 and in PCA (Portland Cement Association) Design and Control of Concrete Mixes.  Then, like an engineer, you will evaluate your concrete and test it for strength.

Project Goals

- Design a concrete mix that can hold 4000 psi with a 3-4 in. slump

- Evaluate the concrete fresh (workability) and hard (strength) properties

What you need

- Concrete mix design – follow the worksheet on the following pages (will need access to computer to complete design)

- Cement (use mix design to determine how much)

- Fine aggregate (sand)

- Coarse aggregate (gravel) – you may need to remove larger rocks

- Water

- Form – either a cylinder or beam mold for testing

- Mixing bowl and spoon

- Access to a concrete compression testing machine (contact local university or concrete company) – or – supports and weights for beam testing

Concrete Mix Design

The first step is coming up with your mix design.  For this we will use the procedures in ACI 211.1 or the PCA Design and Control of Concrete Mixtures.  This website (https://concrete.union.edu/general.htm) also uses the same procedure so you can complete the design following the steps in the website.  We will be using the absolute volume method, US units, and Non air-entrained. The absolute volume method assumes you are making 1 cubic yard (or 27ft3) of concrete.  It finds the volumes of cement, water, air, and coarse aggregate. The amount of fine aggregate is the space left over.

On the first page select: Absolute volume, US units, and Non-air entrained then click the button “Start the Design Process”

Enter the maximum slump = 4 in. and minimum slump = 3 in. in step 1

Slump.   Slump is a measure of concrete consistency.  It is related to the workability of concrete (or how fluid it is for placing and finishing).  Higher slumps indicate a more fluid concrete and lower ones indicate concretes that are stiffer.  Most normal concretes use a slump of 3-4 inches so we will use a maximum of 4 in. and minimum of 3 inches in our design

- The nominal maximum aggregate size is the approximate size of the largest aggregate (if the aggregate can fit through a sieve (or grate) with a certain size opening.  If you have a typical gravel then the maximum size is usually ¾ inch.  If you are using a smaller gravel (pea gravel) you can use 3/8 inch.

Enter the maximum size of your coarse aggregate in step 2.  (usually ¾ or 3/8 in.)

- Mixing water and air content are given from an empirical table developed by ACI that works for most concretes across the U.S.  Remember concrete mix design is a trial-and-error process.  This table just gives a good starting point.  Using the slump and maximum aggregate size determined in the previous steps find the amount of mixing water.

We will be using a non air-entrained concrete.  That means it does not have extra air bubbles in it to help with freeze-thaw damage which is typical of interior concretes.

Volume of Water= Weight of water62.4 lb/ft3

Volume of air=% air*27 ft3

Read from the table to determine your amount of mixing water and air content.  Enter these values and clock the “compute” button.

- The water-cement ratio is the primary ratio that controls the strength of the concrete.  4000 psi is a typical strength for normal concretes.  We want a non air-entrained concrete so find the correct water-cement ratio according to the table. (There is a table for maximum water-cement ratios for concrete exposed to freezing and thawing – we will ignore these).

Weight of cement= Weight of waterwater-cement ratio

Volume of Cement= Weight of cement3.15*62.4 lb/ft3

We won’t be using any pozzolanic material (supplementary cementitious material) like fly ash or silica fume so proceed with the next step.

Read from the table to determine your water cement ratio based on the desired compressive strength.  Enter these values and the value of 3.15 for the specific gravity of cement and click the “compute” button.

- Coarse aggregate amount is determine based on the fineness of the fine aggregate and the size of the coarse aggregate.  The fineness of the fine aggregate (sand) is determined from a sieve analysis and given a value from 2.4 to 3.2 with finer fine aggregate having lower values.  In our mix we are going to assume a fineness modulus of 2.6 which is typical of what you would see with play sand from a hardware store.  The table will give you the ratio of the bulk coarse aggregate volume to the total volume of the concrete.  The unit weight of the coarse aggregate is typically about 100 lb/ft3.  The specific gravity is typically about 2.55 for most limestone gravels in Missouri.

Weight of coarse aggregate= ratio*27ft3*100lbft3

Solid volume coarse aggregate= Weight of coarse aggregate2.55*62.4 lb/ft3

Display your maximum aggregate size.  Then enter a value of 100 ;b/ft3 for the unit weight of the coarse aggregate, and 2.6 for the fineness modulus of the fine aggregate.  Then read from the table the volume of coarse aggregate per unit volume of concrete and enter this value.  Finally enter the specific gravity of 2.55 and click the “compute” button.

- Fine aggrege fills the rest of the cubic yard volume.  Most sands in Missouri have a specific gravity around 2.6.

Volume fine aggregate=27ft3-volume of cement-volume of air-volume of coarse aggregate

Weight of fine aggregate= Volume of fine aggregate*2.6*62.4 lb/ft3

Enter the specific gravity of the fine aggregate of 2.6.  Then click the “compute” button.

- Next we have to adjust for the moisture content in the aggregates. Think of aggregate like little sponges.  If they are dry, they will suck water out of our concrete mix and it will not be available for the hydration process.  So, we have to add extra water in the mix just for the aggregate to absorb.  This is done by knowing both the moisture content – how much moisture the aggregate already has, and the absorption – how much moisture the aggregate will absorb to be completely saturated.  The moisture content varies on a daily basis with the weather, but if our aggregates are stored indoors, it should be fairly low.  So, use a moisture content of 0.2% for both the coarse and fine.  The typical absorption values are 1.5% for fine and 4% for coarse.  Therefore, we can determine the net mixing water that includes the water needed for the aggregate to absorb.  We can also adjust the actual weights of the coarse and fine to account for the moisture in them.  (In our case there is so little moisture it doesn’t make much difference)

Net mixing water=Design mix water+weight of coarse agg*0.04-.002+weight of fine agg*(0.015-.002)

We will not be using any admixtures in this mix design.

Enter the following:

Moisture content coarse aggregate = 0.002

Moisture content fine aggregate = 0.002

Absorption coarse aggregate = 0.04

Absorption fine aggregate = 0.015

Then click the “compute” button

- The last step is to adjust to our batch size.  We will not be making an entire cubic yard of concrete!  How much you make depends on the forms that you are using.

Option 1 – cylinders for testing.  If using 3x6 in. cylinders then the volume is 6 in. * 1.5 in.2* = 42.4in3.  Therefore for 2 cylinders and about 10% extra you will need a batch size of 93 in3 or 0.054 ft3.  That is 0.2% of a cubic yard.

Option 2 – Making a beam.  Compute the volume of your beam and find the needed % of a cubic yard.  For example, if you are making a 1 in. x 1in. x 12 in. beam you will need 12 in3 of concrete or 0.026% of a cubic yard.

Enter your batch size in percentage of a cubic yard and click the “summarize” button.

Record your final mix design here:

Weight of cement =          lb

Weight of water =           lb

Weight of coarse aggregate =           lb

Weight of fine aggregate =            lb

Follow these steps to make and test your concrete!

- Batch the concrete

Now that you have determined the mix design now it is time to batch the concrete.  Weight out everything that is needed, and then mix in a bucket or bowl (depending on how much concrete you are making).  Wet any equipment that you have prior to mixing to aid in cleanup.  Add the water slowly to make sure you are not adding too much (see step 2). Make sure the concrete is mixed thoroughly.

Step 1 – Weigh out your coarse and fine aggregate, sand, and water.  Mix it all together

- Evaluate the concrete

Once the concrete is mixed, evaluate the fresh properties.  Does it seem fluid enough?  Or is it too runny?  Remember the mix design procedure that we just did is just the starting point to a trial-and-error procedure.  Sometime you can tell the mix design is not quite right just by looking at the fresh properties.  Engineers have specific tests to evaluate the slump, air content, and temperature when the concrete is fresh.  We can’t evaluate these without the equipment, but you can determine if the concrete consistency is good.

You can make adjustments to your design now if you wish.  If the concrete is too stiff add a little more water (but be careful a little water goes a long ways).  If the concrete is too runny add a little more cement.  Make note of how you changed your design so you can make the same mix again in the future.

When you are done make sure you clean everything.  Concrete is way easier to clean when it is still fluid.  You may want to wear gloves for the mixing.  Concrete is very alkaline (opposite of acid) and will dry out the skin.  Make sure you wash your hands well when finished.

Step 2 – Evaluate the concrete.  This concrete was a little too runny when all the water was added so more cement was added.

- Fill up the forms

Now you can fill your forms.  If you are doing cylinders fill half-full, then rod the layer (insert and remove a metal rod quickly). This will help consolidate the concrete.  The finish filling, rod, and level off.  If you are doing a beam, go ahead and fill it up, but tap the sides and bottom to help consolidate.  You want to remove any large pockets of air.  Level it off so you have a nice smooth top.

Step 3 – Fill the form.  This form is a 1 in. by 1 in. by 12 in. beam.

- Let it cure

Concrete hardens through a reaction with water and cement.  We need to make sure the water sticks around for this reaction to occur.  Cover your cylinders or beams with plastic to help keep the moisture in.  Engineers use special curing rooms that keep concrete moist while it cures.    We usually use the 28-day mark as the reference mark for concrete strength, although it continues to get hard forever.  If you want to test earlier, you can, but it may not be full strength.

- Test the concrete

Remove the concrete from the forms and test it.

Option 1 – Cylinders.  Cylinder testing is the most common and accurate way to determine concrete compressive strength.  If you made cylinders you will have to take them to a testing lab to determine the compressive strength.  For a 3 in. diameter cylinder with a target strength of 4000 psi, it will take almost 30,000 lbs to break it….that is a much as an empty semi-truck!

Area*stress=load

3in22*π*4000psi=28,274 lbs

Option 2 – Beams.  If you make beams, you can test the concrete in bending because concrete is much weaker in tension than compression.  Remember, bending causing compression at the top and tension at the bottom.  This will allow you to test the beams in your classroom, but is not quite as accurate as cylinder testing.  Using some simple equations of mechanics, you can evaluate your concrete strength.  You will need to know your span length (length between supports), beam width (b) and height (h).

Bending Moment=Load*span length4

Flexural stress= Moment*h/2I

For a rectangular section I=bh312

So stress = tensile stress= Load*span length4*h2I

For a 1in. by 1in. beam with a span length of 10 in. The stress would be 15*load.

The tensile strength of concrete is about 10% of the compressive strength.  So, if we were aiming for a 4000 psi concrete, then the tensile strength would be 400 psi, and the load required to fail the beam would be 26.6 lbs.   Test out your concrete and see if it can carry this load!

Beam Testing

Beam set up for testing with 10 in. span length

20 lbs

10 lbs

5 lbs

3 lbs

Load the beam incrementally to determine how much it can carry.  In this case cans (about 1lb each) and hand weights were used.  Use whatever material you have on hand to load the beam.  Alternatively, you can pull down on the beam by hanging weights or using a pull scale.

30 lbs

25 lbs

The beam held 25 lbs, but failed at 30 lbs – which was pretty close to our 26 lb goal!

Evaluate the concrete

Answer these questions about your concrete

- How easy was it to mix and work with your concrete?  Remember concrete has to be placed in its fluid state.  Adding extra water makes it easier to work with but reduces the strength.  Would you want to use this concrete on a job site?  What changes could be made to the mix design to make it easier to work with?

- What was your concrete strength (compressive strength or weight carried)?  Did you come close to the 4000 psi goal?  What changes could you make to your mix design to increase the strength (would these also impact the workability)?

- Think about the failure of your concrete – was it sudden?  What do you think the effect of adding reinforcement (steel bars or fibers) would be in your concrete?  Would this help prevent the sudden failure?

Teacher Notes:

Prepare ahead of time

- Make sure you have enough supplies (first page) for all students.  Students can work in groups.  You may need to run the design yourself to determine the approximate amounts of cement and sand.  The cement is available at any hardware store (Lowes, Home Depot, etc.).  Look for Type I/II cement (not the premixed stuff with aggregate in it – no quickcrete or “concrete mix” for example https://www.homedepot.com/p/Ash-Grove-92-6-lb-Portland-Cement-Concrete-Mix-100-92-AG/202075616)  They are typically in 90 lb bags for about $18 (you will have plenty of leftover).  Any playground or similar sand will do.

- Print out copies of instructions

- To complete mix design students will need web access on a computer or their phones

- This is a multi-day activity.  The concrete will need at least one day (the longer the better – suggested time is one week) to cure before testing.

Introduce the challenge (20 min video + 5 min discussion)

- Show the video on concrete mix design and hydration.

- Talk with students about: Where do we use concrete?  What concrete is composed of?  What are the goals in our concrete mix design (is it just about strength)?  How do we evaluate concrete?

- Go over activity instructions and goals.

Design concrete mix (20 min)

- Give students about 20 min to complete the concrete mix design.

- Let them compare the mix designs with other groups.  If they are all trying for the same strength and using the same assumed properties, they should all have the same answers.  Part of engineering is double checking work and having others review the work.  Consider letting students share the design with another group to see if there are any mistakes.

Mix concrete and pour into forms (30 min)

- Have the students mix the concrete according to the instructions provided.  Concrete is alkaline which can dry out skin for a short exposure and lead to chemical burns for prolonged exposures.  If the students touch the concrete, make sure the students wash hands soon after handling concrete or wear gloves.

- Make sure they evaluate the concrete before they pour it – is it at the right consistency?

- Put the specimens someplace safe to cure overnight to one week.

Test the beams or cylinders (30 min)

- Time to test your beams or cylinders!  Follow the instructions provided to determine who made the strongest concrete!

Discussion (15 min)

- Ask some of these questions to help students think about their design.

- How easy was it to mix and work with your concrete?  Remember concrete has to be placed in its fluid state.  Adding extra water makes it easier to work with but reduces the strength.  Would you want to use this concrete on a job site?  What changes could be made to the mix design to make it easier to work with?

- What was your concrete strength (compressive strength or weight carried)?  Did you come close to the 4000 psi goal?  What changes could you make to your mix design to increase the strength (would these also impact the workability)? (decreasing the water/cement ratio will increase the strength but make the concrete harder to work with)

- Think about the failure of your concrete – was it sudden?  What do you think the effect of adding reinforcement (steel bars or fibers) would be in your concrete?  Would this help prevent the sudden failure?

Optional – Inquiry based learning questions.

- Your class is asked to determine a mix design for a new sidewalk at your school.

- Design your concrete.

  - What would be the goals of your concrete mix design – strength, workability, setting time….etc?

  - How would you evaluate the concrete properties?

  - Design a concrete mix that you think will meet the desired goals.

- Conduct experiment and record data.

  - Mix your concrete and make beams or cylinders.

  - As you are mixing evaluate the fresh concrete properties – would this concrete be easy to pour and finish for a sidewalk?

  - Let the concrete cure and test the strength of the concrete – is the strength of the concrete important for a sidewalk?

- Analyze and interpret results.

  - What was good or bad about the concrete you made.  How would you change the mix design to improve the concrete?

- State conclusions

  - Which design would you recommend for the sidewalk?